This specification is provided by Mid-Atlantic Coatings, Inc. as a service to owners and engineers and is intended to be used as a guideline for preparing a project specific specification section.  Every heading may not be needed.  Delete headings not used and renumber remaining used headings to be numerically in correct.

PART 1 – GENERAL

  - DESCRIPTION

    - Scope:

      - CONTRACTOR shall provide all labor, materials, equipment and incidentals as

specified, shown, and required to furnish and install the protective liner for concrete Work.

      - Where not otherwise shown, extent of the protective lining shall be located 1) interior walls of the structures and manholes to be protected and, 2) interior surface of lids and top slabs (soffits) of structures to be protected.  Without restricting volume or generality, work to be performed under this section may include, but is not limited to:

        - Hydrogen Sulfide Gas and Sulfuric Acid Environments

        - Headworks

        - Grit Chambers

        - Wet Wells

        - Digesters (Mesa and Therma)

        - Lift Stations

        - Concrete Pipes

        - Clarifiers

      - Types of protective lining for concrete Work required include, but are not necessarily limited to, the following:

a.  	Trowelable, fast-setting, cementitious shallow-depth overlay (resurfacer)

b.	Trowelable, fast-setting, epoxy- modified cementitious thin overlay (parge coat)

c.	Corrosion-resistant, spray-applied, fiber-reinforced high-build epoxy lining

(basecoat)

d.	Corrosion-resistant, high-build epoxy glaze coat (topcoat)

e.	Miscellaneous materials.

      - Cleaning, surface preparation, lining application, and thicknesses shall be as specified

herein and shall meet or exceed the lining manufacturer’s recommendations.  When the

manufacturer’s minimum recommendations exceed the specified requirements,

CONTRACTOR shall comply with the Manufacturer’s minimum recommendations.

    - Coordination:

      - Coordinate surface preparation of substrates to avoid later difficulty or delay in

performing the Work of this Section.

      - Review installation procedures under other Sections and coordinate the instillation of

items that must be installed prior to application of the protective lining.

      - All substrate surface preparation and lining application, including concrete resurfacing, to be completed by manufacturer’s approved Applicator.

      - The CONTRACTOR shall coordinate with ENGINEER regarding the availability of work areas, completion times, safety, access and other factors which can impact plant operations.

    - Related Sections:

      - Section 01300, Submittals

      - Section 03300, Cast-in-Place Concrete

      - Section 07150, Sealants

      - Section 07160, Bituminous Damproofing

1.2   	REFERENCES

A.	This Section contains references to the governing standards and documents listed below.  They are a part of this Section as specified and modified; the current version shall apply unless otherwise noted.  In case of conflict between the requirements of this section and those of the listed documents, the more stringent of the requirements shall prevail.

1.	American Concrete Institute, (ACI)

a.	ACI 301  – Specifications for Structural Concrete

b.	ACI 308R  – Guide to Curing Concrete

c.	ACI 350 –  Code Requirements for Environmental Engineering Concrete 			Structures and Commentary.

d.	ACI 515 – A Guide to the use of Waterproofing, Damproofing, Protective, and

Decorative Barrier Systems for Concrete.

e.	ACI 546.R  – Concrete Repair Guide

f.	ACI 546.3R  – Guide for the Selection of Materials for the Repair of Concrete

2. 	ASTM International, (ASTM)

        - ASTM C 868 – Standard Test Method for Chemical Resistance of Protective Linings

        - ASTM D 2794 – Standard Test Method for Resistance of Organic Linings to the Effects of Rapid Deformation (Impact)

        - ASTM D 4060 – Standard Test Method for Abrasion Resistance of Organic Linings by the Taber Abraser

        - ASTM D 4285 – Standard Test Method for Indicating Water or Oil in Compressed Air

        - ASTM D 4263 – Standard Test Method for Indicating Moisture in Concrete by the Plastic Sheet Method

        - ASTM D 4414 – Standard Practice for Measurement of Wet Film Thickness by Notch Gages

        - ASTM D 6944 Standard Test Method for Measuring Humidity with a Physchrometer

        - ASTM F 1869 – Standard Test Method for Measuring Moisture Vapor Emission Rate of Concrete Subfloor Using Anhydrous Calcium Chloride

        - ASTM F 2414 – Standard Practice for Sealing Sewer Manholes Using Chemical Grouting

3.	International Concrete Repair Institute, (ICRI)

a.   	Guideline No. 03730 – Guide for Surface Preparation for the Repair of Deteriorated Concrete Resulting from Reinforcing Steel Corrosion

b.	Guideline No. 03732 – Selecting and Specifying Concrete Surface Preparation for Sealer, Linings, and Polymer Overlays

4.	NACE International, (NACE)

a.	NACE Publication 6D-173 – A Manual for Painter Safety

b.	NACE SP0188 – Standard Practice for Discontinuity (Holiday) Testing of

Protective Linings

c.	NACE SP0892 –  Standard Practice for Coatings and Linings over Concrete for Chemical Immersion and Containment Service

d.	NACE No. 6/SSPC-SP13 – Surface Preparation of Concrete

      - Occupational Safety and health Administration, (OSHA)

        - Safety and health Standards (29 CFR 1910/1926)

      - SSPC: The Society for Protective Linings, (SSPC)

        - SSPC-SP13/NACE No. 6 – Surface Preparation of Concrete

        - SSPC-Guide 12 – Guide for Illumination of Industrial Painting Projects

      - Standard Practice for the Rapid Evaluation of Coatings and Linings by Severe Wastewater Analysis Test, (S.W.A.T.)

    - Unless otherwise specified, references to documents shall mean the documents in effect at the time of receipt of Bids.  If referenced documents have been discontinued by the issuing organization, references to those documents shall mean the replacement documents, the last version of the document before it was discontinued.

1.3 	QUALITY ASSURANCE

- Applicator Qualifications:

      - Engage a surface preparation and lining installation Applicator with specific knowledge and experience in the application of the type of protective lining specified, and who agrees to employ only tradesmen with specific skill and experience in this type of Work.  Submit firm and qualifications of proposed Applicator to ENGINEER for approval.

      - Establish quality control procedures and practices to monitor phases of surface preparation, storage, mixing, application, and inspection throughout the duration of the project.  Provide a fulltime, onsite person whose responsibilities will include quality control of the linings system.

      - Quality control procedures and practices must include the following items:

a.	Training of personnel in the proper surface preparation requirements.

b.	Training of personnel in the proper storing, mixing, application, and inspection of the linings.

c.	Training of personnel in health and safety practices.

4. 	All Applicators shall be approved by the protective lining materials manufacturer.

        - Application equipment shall be acceptable to the lining manufacturer.

- Performance Criteria:  The surfaces to receive the protective lining shall be capable of withstanding, under constant exposure to, raw wastewater, permeation from hydrogen sulfide and other sewer gases, and attack from organic acids generated by microbial sources, with no adverse effects.  Products must have sufficient field history and accelerated laboratory testing to substantiate product viability for these exposures.

- Source Quality Control:  Provide each component of protective lining produced by a single manufacturer, including recommended repair overlay (resurfacers), base coat and top coat materials.

- Reference Standards:  Comply with applicable provisions and recommendations of all standards listed in Section 1.2 except as otherwise shown or specified.

- Protective Linings system specified are as manufactured by Tnemec Company, Inc., Kansas City, MO (816) 483-3400.  Specified system is the minimum standard of quality for this project.  Request for material substitutions shall be in accordance with requirements of the project specifications.

  - SUBMITTAL

A.	In accordance with the procedures and requirements set forth in the General Conditions and Section 01200 entitled “Submittals”, the CONTRACTOR shall submit all required information as specified herein.

B.	Shop Drawings:  Submit for approval prior to commencing any Work:

1.	Product Data Sheets:  Copies of current technical data for each component specified and

applied as outlined in this Section.

2.	Material Safety Data Sheets:  Copies of current MSDS for any materials brought on-site including all solvents and lining materials.

3.	Performance Testing Reports:  Copies of test data for the entire physical, chemical, and permeation properties listed herein and as outlined within this Section.

4.	Instillation Instructions:  Manufacturer’s written installation instructions for the materials specified in this Section.

5.	Construction Details:  Copies of manufacturer’s computer generated standard lining details for specified materials, including: leading edge termination, metal embedment in concrete, joint detail, wall-to-slab detail, pipe termination detail, and any other detail at the request of the ENGINEER.

C.	JOBSITE REPORTS:

1.	Submit at the completion of work.

2.	Daily Reports:  Include surface preparation, substrate conditions, ambient conditions application procedures, lining materials applied, material quantities, material batch number(s), description of work completed and location thereof.

1.5   	PRODUCT, DELIVERY, STORAGE AND HANDLING

A.	Delivery of Materials:

1.	Deliver material in manufacturer’s original, unopened and undamaged packages.

2.	Clearly identify manufacturer’s, brand name, contents, color, batch number, and any

personal safety hazards associated with the use of or exposure to the materials on each

package.

3.	Packages showing indications of damage that may affect condition of contents are not

acceptable.

B.	Storage of Materials:

1.	Materials shall be stored in accordance with manufacturer's recommendations in enclosed structures and shall be protected from weather and adverse temperature conditions.  Flammable materials shall be stored in accordance with state and local codes.  Materials exceeding storage life as defined by the manufacturer shall be removed promptly from the site. Store all materials only in area or areas designated by the ENGINEER solely for this purpose.

2.	Store in original packaging under protective cover and protect from damage.

3.	Stack containers in accordance with manufacturer’s recommendations.

C.	Handling of Materials:  Handle materials in such a manner as to prevent damage to products or

finishes.

1.6 	JOB CONDITIONS

A.	Environmental Requirements:

1.	Maintain substrate temperature and ambient temperature before, during and after installation above 50°F (10°C) and rising in accordance with protective lining material manufacturer’s instructions.

2.	Provide adequate ventilation during instillation and full curing periods of the protective lining.

3.	Protective Lining shall not be applied when ambient air temperature is within 5°F (3°C) of the dew point and falling.

4.	Protective Lining shall not be applied when relative humidity is outside of material manufacturer’s recommendations.  Do not prepare surfaces or apply materials in rain, snow, fog, mist, or otherwise inclement weather as per material manufacturer’s instructions.

B.	Dust and Contaminants:  Protect work and adjacent areas from excessive dust and airborne

contaminates during protective lining application and curing. Schedule Work to avoid

excessive dust and airborne contaminants.

  - WARRANTY

- Protective Lining Manufacturer shall warranty its products as free from material defects for a

minimum period of three (3) years.  Provide associated Warranty Certificate.

B.	CONTRACTOR shall warranty the installed protective lining system as free from workmanship defects for a minimum period of three (3) years.

PART 2 - PRODUCTS

  - MATERIAL

    - Protective Lining shall be comprised of 1) concrete replacement or underlayment, 2) spray-applied, fiber-reinforced epoxy liner (basecoat), and 3) epoxy glaze (topcoat).

      - Cementitious Underlayment: Epoxy-polymer modified cementitious thin overlay

(underlayment) applied to new or existing concrete to a depth up to 1/2-inch. Repair new or existing concrete and provide level substrate for application of the protective lining; and

      - Spray-applied, fiber-reinforced high-build epoxy liner (basecoat) to provide a chemical,

permeation, and abrasion resistant protective lining against physical and chemical attack

phenomena typically associated with municipal wastewater headspace conditions; and

      - Epoxy glaze coat (topcoat) to provide enhanced chemical, permeation, and abrasion

resistance.

    - CONTRACTOR shall provide all accessory components such as polysulfide sealants, and curing compounds, as recommended by the manufacturer for maximum protective lining adhesion to substrate, and long-term service performance.

    - Epoxy modified Cementitious Underlayment:

      - Product: Tnemec Series 218 Mortar Clad

      - Properties

        - Minimum thickness 		1/16 inch

        - Maximum thickness		1/2 inch

        - Application Time

Working Time at 75°F 		60 min

Initial set at 75°F: 	90 min

        - Bond Strength (ICRI 03739)

Applied at ¼” to Concrete           		Concrete Failure

        - Applied at 2.0” to Concrete           		Concrete Failure

        - Compressive Strength                    		5,137 psi

        - Curing Requirements (ACI 308)

Method:		Ambient Cure

Duration:                                 		15 hours

    - Epoxy Lining, Fiber-Reinforced Protective Lining (Basecoat & Finish):

      - Product: Tnemec Series 436 Perma-Shield

      - Properties

        - Application Time at 75°F             			30 min

        - Color	Gray

        - Minimum Dry Film Thickness (DFT)	80 mils

        - Maximum Dry Film Thickness (DFT)	125 mils

        - Severe Wastewater Analysis Test (S.W.A.T.)

Initial EIS Impedance (Log Z0.01 Hz Ω cm2)          10.4

Final EIS Impedance (Log Z0.01 Hz Ω cm2)   	10.2

Optical Microscopy                                         No more than 16%

Tensile Strength                                            	No more than 12%

Flexural Strength                                          	No more than 11%

        - Bond Strength (ASTM D7234)

Bare Concrete/Series 436                                	Concrete Failure

Bare Concrete/Series 215/Series 436               	Concrete Failure

Bare Concrete/Series 218/Series 436               	Concrete Failure

        - Chemical Resistance (ASTM C686)

25% H2SO4, 100 days, 100°F                         	No effect

        - Compressive Strength (ASTM D695)                    	8,866 psi

        - Elongation (ASTM D638)                                      7.65%

        - Flexural Strength (ASTM D790)	8,148 psi

Modulus of Elasticity	5.4 x 105 psi

        - Shrinkage (ASTM C531)	0.06%

        - Tensile Strength (ASTM D2370)	2,940 psi

        - Thermal Expansion

Linear Coefficient (ASTM C531)                    5.68 x 10-5 in/in/°F

Thermal Cycling (ASTM D6944)                    	No effect

        - Water Absorption (ASTM C413)	0.4%

        - Water Vapor Transmission (ASTM D1653)          	1.62 g/m2 /24 hr

    - Epoxy Lining, Glaze Protective Lining (Optional Topcoat): *See Spec Writer Note Below

      - Product: Tnemec Series 435 Perma-Shield

      - Properties	:

        - Application Time at 75°F                                      	30 min

        - Color	Gray

        - Minimum Dry Film Thickness (DFT)	15 mils

        - Maximum Dry Film Thickness (DFT)	20 mils

        - Severe Wastewater Analysis Test (S.W.A.T.)

Initial EIS Impedance (Log Z0.01 Hz Ω cm2)         	11.3

Final EIS Impedance (Log Z0.01 Hz Ω cm2)   	11.1

Optical Microscopy                                         	No more than 9%

Tensile Strength                                               No more than 19%

Flexural Strength                                             	No more than 6%

        - Bond Strength (ASTM D7234)

Bare Concrete/Series 436                                	Concrete Failure

Bare Concrete/Series 215/Series 436               	Concrete Failure

Bare Concrete/Series 218/Series 436              	Concrete Failure

        - Chemical Resistance (ASTM C686)

25% H2SO4, 100 days, 100°F                        	No effect

        - Compressive Strength (ASTM D695)                    	9,427 psi

        - Elongation (ASTM D638)                                    	14.1%

        - Flexural (ASTM D790)

Strength                                                           	3,289 psi

Modulus of Elasticity	3.0 x 105 psi

        - Tensile Strength (ASTM D2370)	2,053 psi

        - Water Absorption (ASTM C413)	0.07%

        - Water Vapor Transmission (ASTM D1653)          	2.27 g/m2 /24 hr

SPEC WRITER NOTE:

Series 435 is an optional topcoat. If not selected delete.

PART 3 - EXECUTION

  - FIELD QUALITY CONTROL, INSPECTION AND TESTING

    - Inspection by the ENGINEER or others does not limit the CONTRACTOR’s responsibilities for quality control inspection and testing as specified herein or as required by the Manufacturer's instructions.

    - CONTRACTOR and his Applicator shall examine the areas and conditions under which the protective lining Work is to be performed in accordance with SSPC-SP13/NACE No. 6 and notify ENGINEER in writing of conditions deleterious or otherwise detrimental to the proper and timely completion of the work.

    - Commencement of the Work of this Section shall indicate that the substrate and other conditions of installation are acceptable to the CONTRACTOR and his Applicator, and will produce a finished product meeting the requirements of the Specifications.  All defects resulting from such accepted conditions shall be corrected by CONTRACTOR at his own expense.

    - Stopping Active Leaks:  After surface cleaning, any visible leaks or other water ingress shall be reported to the ENGINEER.  Any water infiltration through minor leaks must be stopped using a polyurethane grout manufactured by Avanti International, Webster, TX (281-486-5600), or approved equal. Surface and grouting material may require additional surface preparation prior to application of protective lining.

    - Existing Concrete:  Inspect and record findings for the degree of cleanliness of substrates used.  The pH of the concrete substrate will be measured using pH indicating papers. The pH testing is to be performed once every 50 sq. ft. Acceptable pH values shall be between 9.0 and 11.0 as measured by a full-range (1-12) color indicating pH paper with readable color calibrations and a scale at whole numbers (minimum).  Use Hydrion Insta-Check Jumbo 0-13 or 1-12 or equal. The paper shall be touched to the surface once using moderate gloved finger pressure. The surface shall not be wiped or moved laterally to disturb the surface during pH testing. Following the one touch, lift the paper vertically to not "wipe" the surface. Compare the color indicated with the scale provided and record the pH. Spot check any areas that may be questionable with phenolphthalein.

3.2   	PREPARATION

A	Concrete surfaces to be coated shall be free of curing compounds and form release agents, laitance and foreign particles that my inhibit bonding.  Prior to start of protective lining systems application, high-pressure water clean, waterjet or abrasive blast surfaces to be covered as required, and inspect the substrate in accordance with SSPC-SP13/NACE No. 6.  Surface preparation procedures shall be in accordance with SSPC-SP13/NACE No. 6 and ICRI Guideline No. 03732.  Surface preparation requirement is to expose aggregate and obtain a uniform surface texture resembling an ICRI-CSP5-6.

B.	All new cast-in-place concrete shall cure for a period of 28 days in accordance with ACI 308 before protective lining system is installed, unless otherwise recommended by the Protective Lining manufacturer.

C.	Concrete surfaces to receive protective lining shall be a Smooth Form Finish as defined in ACI 301.  Surfaces shall not be rubbed, sacked, troweled or otherwise finished in any manner that will obscure or cover the firm substrate surface.

D.	Level or grind concrete substrates to manufacturer’s recommended tolerances and produce a smooth, uniform installation, including removal of all sharp edges, ridges, or depressions.

E.	New Concrete Application:  Voids, bugholes, and other surface depressions shall be filled with specified underlayment material, re-establishing plan finished grades and concrete planes.

      - Inspect and record substrate profile (anchor pattern).  Surfaces shall be abraded, at a minimum, equal to the roughness of CSP5 in accordance with ICRI Guideline 03732 and SSPC-SP13/NACE No. 6.

    - Existing Concrete Application:  Existing concrete structures to receive protective lining system must be capable of withstanding imposed loads and stresses.  All oil, grease and chemical contaminants must be removed from the surface of concrete by chemical cleaning prior to preparation in accordance with SSPC-SP13/NACE No. 6. Surfaces must be firm, free of standing water, laitance, form release agents, and be structurally sound.  CONTRACTOR shall verify that the pH of the cleaned concrete surfaces to be coated is within the range of to 9 to 11.  Application of coating materials outside this range will not be permitted without written approval from the ENGINEER.

      - Inspect and record substrate profile (anchor pattern).  Surfaces shall be abraded, at a minimum, equal to the roughness of CSP5 in accordance with ICRI Guideline 03732 and SSPC-SP13/NACE No. 6.

3.3   	APPLICATION

A.	Protective Lining system shall be installed when surface temperature is between 50-130°F (10-54°C).  The material should be conditioned between 70°F (21°C) and 80°F (27°C) prior to application.

B.	Application in direct sunlight and/or with rising surface temperature is not allowed, as this may result in blistering of the materials due to expansion of entrapped air or moisture in the concrete.  In such cases, it will be necessary to postpone the application until later in the day when the temperature of the substrate is falling.

C.	Areas not to receive Protective Lining System shall be masked or otherwise protected to prevent these surfaces from being coated.

D.	Ensure straight, even termination of protective lining system on wall edges and flush with embedded steel.

  - ACCEPTANCE CRITERIA

A.	All surfaces shall be prepared in accordance with the specification and referenced standards herein.

  - ADJUSTMENTS AND CLEANING

A.	At the completion of the Work, CONTRACTOR shall remove all materials and debris associated with the Work of this Section.

B.	Clean all surfaces not designated to receive protective lining.  Restore all other wok in a manner acceptable to ENGINEER.

C.	All finished protective lining shall be protected from damage until Final Acceptance of the Work.  Protective lining damaged in any manner shall be repaired or replaced at the discretion of ENGINEER, at no additional cost to OWNER.

D.	Clean all protective lining as recommended by the manufacturer to provide finished Work acceptable to OWNER, just prior to Final Acceptance.

END OF SECTION