SPECIFIER NOTE

This specification is provided by Mid-Atlantic Coatings, Inc. as a service and is intended to be used as a guideline for preparing a project specific specification section.  Every heading may not be needed.  Delete headings not used and renumber remaining used headings to be numerically correct. Contact Mid-Atlantic Coatings or Tnemec Company before using this specification for any Overcoat Project.

PART 1 - GENERAL

      - RELATED DOCUMENTS

        - This Section includes shop and field surface preparation and shop and field painting of various substrates.

          - Surface preparation, including in the shop and applications of metal primer, and field applications of primers and finishes are specified in this Section.

        - Drawings and general provisions of the Contract, including General and Supplementary Conditions and Division 1 Specification Sections, apply to this Section.

      - SUMMARY

        - This Section includes surface preparation and application of high-performance coating systems on the following substrates:

          - Exterior Substrates:

            - Aged Shop Coated Panels.

        - Related Sections include the following:

          - Division 5 Sections for shop priming of metal substrates with primers specified in this Section.

          - Division 9 Section "Painting" for general field painting.

      - SUBMITTALS

        - Product Data:  For each type of product indicated.

        - Samples for Initial Selection:  For each type of finish-coat product indicated.

        - Samples for Verification:  For each type of coating system and in each color and gloss of finish coat indicated.

          - Submit Samples on rigid backing, 8 inches square.

          - Step coats on Samples to show each coat required for system.

          - Label each coat of each Sample.

          - Label each Sample for location and application area.

        - Product List:  For each product indicated.  Cross-reference products to coating system and locations of application areas.  Use same designations indicated on Drawings and in schedules.

      - QUALITY ASSURANCE

        - Material Performance Criteria:

          - Products:  Provide certified test reports when submitting products other than those specified herein the specification. Test reports shall indicate the test method, system and requirements for those products being submitted, and shall meet or exceed the test criteria and performance values of the specified coatings herein.

        - Applicator Qualifications:

          - Preparation and Workmanship:  A firm or individual with a minimum of (5) years experienced in applying coatings similar in material design, and extent to those indicated for a particular project, whose work has resulted in applications with a record of successful in-service performance.

        - Mockups:  Apply benchmark samples of each coating system indicated to verify preliminary selections made under sample submittals and to demonstrate aesthetic effects and set quality standards for materials and execution.

          - Architect will select one surface to represent surfaces and conditions for application of each type of coating and substrate.

            - Provide samples of at least 25 sq. ft.

            - Other Items:  Architect will designate items or areas required.

          - Apply benchmark samples after permanent lighting and other environmental services have been activated.

          - Final approval of color selections will be based on benchmark samples.

          - If preliminary color selections are not approved, apply additional benchmark samples of additional colors selected by Architect at no added cost to Owner.

          - Approved mockups may become part of the completed Work if undisturbed at time of Substantial Completion.

      - DELIVERY, STORAGE, AND HANDLING

        - Deliver materials to project site in manufacturer’s original, unopened packages and containers bearing manufacturer’s name and label and the following information.

          - Product name or title of material.

          - Product description (generic classification or binder type)

          - Manufacturer’s stock number and date of manufacture.

          - Contents by volume, for pigment and vehicle constituents.

          - Thinning instructions.

          - Application instructions.

          - Color name and number.

          - VOC content.

        - Store materials not in use in tightly covered containers in well-ventilated areas with ambient temperatures continuously maintained at not less than 45 deg F.

          - Maintain containers in clean condition, free of foreign materials and residue.

          - Remove rags and waste from storage areas daily.

      - PROJECT CONDITIONS

        - Apply coatings only when temperature of surfaces to be coated and surrounding air temperatures are between 50 and 95 deg F.

        - Do not apply coatings in snow, rain, fog, or mist; when relative humidity exceeds 85 percent; at temperatures less than 5 deg F above the dew point; or to damp or wet surfaces.

  - PRODUCT WARRANTY

- A.	Provide manufacturer’s (10) year color and gloss, crack, check, peel warranty at the completion of the project. For additional years of coverage contact Tnemec Company.

- PRODUCTS

      - MANUFACTURERS

A.	Materials specified are those that have been evaluated for the specific service on this project.  Products of the Tnemec Company, Inc. are listed to establish a standard of quality.  Equivalent materials of other manufacturer's may be submitted a minimum ten days prior to bid date on written approval of the Architect.

B.	Materials specified herein shall not preclude consideration of equivalent or superior materials.  Requests for substitution shall be submitted to the architect a minimum ten days prior to bid date in accordance with the general construction documents and in compliance with substitution procedures in Section 01 60 00 of this Project Manual.

          - Requests for substitution shall include evidence of satisfactory past performance on

- substrates that are listed herein.

          - Substitutions will not be considered that change the generic type, number of coats or do not meet specified total dry film thickness.

- C.	Colors:  As selected by Architect from manufacturer's full range.

      - HIGH PERFORMANCE COATINGS GENERAL

        - Materials Compatibility: Provide shop and field primers, and finish-coat materials that are single source and compatible with one another and with the substrates indicated under conditions of service and application, as demonstrated by manufacturer based on testing and field experience.

      - EPOXY METAL PRIMER & INTERMEDIATE COATING

        - Tnemec Series 27 WB Typoxy (Spot Primer and Intermediate Coat)

- 1.		Generic Type:  Inorganic Hybrid Water-Based Epoxy

- 2.		Finish: Flat

- 3.		Properties:

- a.	Solids by Volume:  90.0 +/- 2.0%

- b.	VOC: 0.10 lbs/gallon (11 grams/litre)

- 4.	Performance Criteria:

- a.	Abrasion: ASTM D 4060, (CS-17 Wheel, 1,000 grams load). No more than 181 mg loss after 1,000 cycles.

b.	Adhesion: ASTM D 4541 (Type V Tester) Not less than 1,440 psi (9.93 MPa)

c.	Cathodic Disbondment: ASTM G8 (1.5V) Classification Group A. No more than

0.018 inch (0.46 mm) disbonded equivalent circle diameter.

d.	Cyclic Weathering: ASTM D 5894. No blistering, cracking, rusting or delamination

of film after 3000 hours continuous exposure

e.	Water Vapor Transmission: ASTM D 1653. No more than 4.68 g/m2 per 24 h water

vapor transmission and no more than 0.22 perms water vapor permeability.

f.	Deionized Water: Continuous immersion in deionized water at 140 F (60 C). No

blistering, cracking, rusting or delamination of film. after 5,000 hours continuous

immersion in deionized water at 140 F (60C).

g.	Salt Spray (FOG). ASTM B 117. No blistering, cracking, rusting or delamination of

film after 6,200 hours.

h.	Hydrostatic Pressure Resistance: ASTM D 7088. No visible leakage on the face of the

block and no blistering after application of 4 lbs pressure for 30 minutes.

  - FLUOROPOLYMER COATINGS

        - Fluoropolymer, Pigmented Coating

- 1.		Product: Tnemec Fluoronar

- 2.		Finishes:

- a.	Series 1070V: Gloss

- b.	Series 1071 or 1071V: Semi-gloss

- c.	Series 1072 or 1072V: Satin

- d.	Series 1078: Metallic

- 3.	Properties:

- a.	Solids by Volume:

- i)		Series 1070V: 51% +/- 2.0% (mixed)

- ii)	Series 1071 & 1072: 60% +/- 2.0% (mixed)

- iii)	Series 1071V: 56% +/- 2.0% (mixed)

- iv)	Series 1072V & 1078: 54% +/- 2.0% (mixed)

- b.	VOC:

- i)		Series 1070V: 0.83 lbs/gallon (99 grams/litre)

- ii)	Series 1071 & 1072: 2.65 lbs/gallon (317 grams/litre)

- iii)	Series 1071V: 0.81 lbs/gallon (97 grams/litre)

- iv)	Series 1072V & 1078: 0.77 lbs/gallon (93 grams/litre)

- 4.	Performance Criteria:

- a.	Abrasion: ASTM D4060, (CS-17 Wheel, 1,000 grams load). No more than 103 mg loss after 1,000 cycles.

- b.	Adhesion: ASTM D 4541 (Method B, Type II Tester). No less than 1,333 psi (9.19 MPa) pull, average of three tests.

- c.	Adhesion: ASTM D 4541 (Method E, Type V Tester). No less than 1,930 psi (13.3 MPa) pull, average of three tests.

- d.	Exterior Exposure: Exposed at 45 degrees facing south. No blistering, cracking, rusting or delamination of film. No less  than 87% gloss retention (8.9 units gloss change) and 2.99 DED FMCII (MacAdam units) color change after 24 months.

- e.	Exterior Exposure: ASTM D 4141, Method C (EMMAQUA). No blistering, cracking or chalking. No less than 96% gloss retention (3.2 units gloss change) and 0.18 DED Hunter Lab color change after 1,260 M/J m2 EMMAQUA exposure, average of five tests in five colors.

- f.	Flexibility: ASTM D 522 (Method A – Conical Mandrel). No less than 14.83% elongation average of three tests.

- g.	Graffiti Resistance: The following graffiti materials applied to coating and allowed to 7 days.

- Reagent  				Series 680 		Xylene		MEK

- Acrylic Spray Paint	Removal		Removal	Removal

- Epoxy Spray Paint	Removal		Removal	Removal

- Markette Marker		Removal		Removal	Removal

- Ball Point Ink			Removal		Removal	Removal

- Crayon				Removal		Removal	Removal

- Lipstick				Removal		Removal	Removal

- Some slight gloss loss and/or softening may occur depending on the amount of effort required for removal of the graffiti and length of exposure of the underlying coating to the cleaning solvents.

- h.	Hardness: ASTM D 3363. No gouging or scratching with an 8H or less pencil.

- i.	Humidity: ASTM D 4585. No blistering, cracking, rusting or delamination of film after 3,000 hours exposure.

- j.	Impact: ASTM D 2794. No visible cracking or delamination of film after 34.6 inch/pounds (3.9J) or less direct impact.

- k.	QUV: ASTM D 4587 (UVA-340 Bulbs, Cycle 4:8 hours UV/4 hours condensation). No blistering, cracking, or chalking. No less than 93% gloss retention (5.7 units gloss change) and 2.21 DED FMCII ( MacAdam Units) color change after 10,000 hours exposure, average of five tests in five colors. No blistering, cracking, or chalking. No less than 60% gloss retention (31.4 units gloss change) and 1.89 DED FMCII              (MacAdam Units) color change after 25,000 hours exposure, average of five tests in five colors.

- l.	Salt Spray (Fog): ASTM B 117. No blistering, cracking, rusting or delamination of film. No more than 1/32 inch rust creepage at scribe after 10,000 hours exposure. No blistering, cracking, rusting or delamination of film. No more than 1/8 inch rust creepage at scribe after 10,000 hours exposure. No blistering, cracking, rusting or delamination of film. No more than 1/16 inch rust creepage at scribe after 10,000 hours exposure.

- m.	Weatherometer Exposure: ASTM D 5031. No blistering, cracking, or chalking. No less than 92% gloss retention (6 units gloss change) and 0.73 DED Hunter Lab Scale color change after 5,000 hours exposure.

- EXECUTION

      - EXAMINATION

        - Examine substrates and conditions, with Applicator present, for compliance with requirements for maximum moisture content and other conditions affecting performance of work.

          - Verify compatibility with and suitability of substrates, including compatibility with existing finishes or primers.

          - Begin coating application only after unsatisfactory conditions have been corrected and surfaces are dry.

          - Coating application indicates acceptance of surfaces and conditions.

      - FIELD PREPARATION

        - Comply with manufacturer's written instructions and recommendations.

        - Shop Coated Metal Panels:

          - Clean using methods recommended in writing by coating manufacturer.

          - Abrasive Blast cleaning shall be done in accordance with SSPC-SP 7, "Brush-Off Blast Cleaning.

          - Abrasive blast cleaning shall be done with a fine abrasive and low pressure psi technique/method.

          - Provide a 25 sq ft area sample area mock-up on the substrate intended for field coating. The sample area shall be done in accordance with specified surface preparation and coating system listed herein and stepped down.

          - After the sample has sufficiently cured provide an adhesion test per ASTM D 3359, Method A & B. If the adhesion rating is less than 4 (5=excellent) contact the coating manufacturer for additional recommendations.

      - APPLICATION

        - Apply high-performance coatings according to manufacturer's written instructions.

          - Use applicators and techniques suited for coating and substrate indicated.

          - Coat surfaces behind movable equipment and furniture same as similar exposed surfaces.  Before final installation, coat surfaces behind permanently fixed equipment or furniture with prime coat only.

          - Coat back sides of access panels, removable or hinged covers, and similar hinged items to match exposed surfaces.

        - Tint each undercoat a lighter shade to facilitate identification of each coat if multiple coats of the same material are to be applied.  Tint undercoats to match color of finish coat, but provide sufficient difference in shade of undercoats to distinguish each separate coat.

        - If undercoats or other conditions show through final coat, apply additional coats until cured film has a uniform coating finish, color, and appearance.

        - Apply coatings by spray application to produce surface films without cloudiness, spotting, holidays, laps, brush marks, runs, sags, ropiness, or other surface imperfections.  Produce sharp glass lines and color breaks.

      - FIELD QUALITY CONTROL

        - Owner reserves the right to invoke the following procedure at any time and as often as Owner deems necessary during the period when coatings are being applied:

          - Owner will engage the services of a qualified testing agency to sample coating material being used.  Samples of material delivered to Project site will be taken, identified, sealed, and certified in presence of Contractor.

          - Testing agency will perform tests for compliance with specified requirements.

          - Owner may direct Contractor to stop applying coatings if test results show materials being used do not comply with specified requirements.  Contractor shall remove noncomplying coating materials from Project site, pay for testing, and recoat surfaces coated with rejected materials.  Contractor will be required to remove rejected materials from previously coated surfaces if, on recoating with complying materials, the two coatings are incompatible.

      - CLEANING AND PROTECTION

        - At end of each workday, remove rubbish, empty cans, rags, and other discarded materials from Project site.

        - After completing coating application, clean spattered surfaces.  Remove spattered coatings by washing, scraping, or other methods.  Do not scratch or damage adjacent finished surfaces.

        - Protect work of other trades against damage from coating operation.  Correct damage by cleaning, repairing, replacing, and recoating, as approved by Architect, and leave in an undamaged condition.

        - At completion of construction activities of other trades, touch up and restore damaged or defaced coated surfaces.

      - HIGH-PERFORMANCE COATING SCHEDULE

        - Exterior Exposed - Aged Shop Coated Vertical Metals

          - Fluoropolymer, Pigmented Coating

            - Spot Primer: Applied Series 27 W. B. Typoxy Primer at 2.-3 mils DFT on all bare and rusted areas.

            - First Coat: Series 27 W. B Typoxy applied at 2.0 to 3.0 mils DFT

            - Finish Coat: Series 1071-color Fluoronar, applied at 2.0 to 3.0 mils [1070V, gloss]  [1071 & 1071V, semi-gloss 1)] [1072 & 1072V, satin 1)]  [1078, metallic 2)]

- SPEC WRITER NOTE

- 1) If the project requires LEED approved products use Series 1071V or 1072V

- 2)  If Series 1078 is selected it must to top-coated with one of the following topcoats; 1079, gloss, 1079-0762, semi-gloss or 1079-0763, satin)

END OF SECTION 09 97 13. 23